# Supplementary Information

for

Dielectric Characterization of Bulk and Pt/ZrO₂/BaTiO₃/ZrO₂/Pt Thin Film Capacitors: Thickness Scaling and Interface Engineering for Energy Storage

Asmin M.K., Smitha P.S., V. Suresh Babu

S1. Additional Experimental Details

### S1.1 Fabrication of BZT Ceramic

Ba(Zr₀.₂Ti₀.₈)O₃ (BZT) powders were prepared using the conventional solid-state reaction method. High-purity BaCO₃, TiO₂, and ZrO₂ powders were weighed according to stoichiometric composition and ball-milled in ethanol for homogenization. The dried powders were calcined at 1000 °C for 4 h to ensure phase formation.

The calcined powder was re-milled, pressed into circular pellets (radius: 4.37 mm), and sintered at 1350 °C for 4 h. Silver paste was coated on both surfaces to form Ag/BZT/Ag capacitors.

## S2. Electrical Measurement Conditions

• Capacitance and dielectric loss were measured over a frequency range of 1 kHz to 1 MHz.

• Leakage current density was measured under DC bias using a source meter.

• All measurements were carried out at room temperature.

## S3. Simulation Parameters (COMSOL Multiphysics)

### S3.1 Thickness-Scaled Ag/BZT/Ag Model

• Dielectric thickness: 104 nm

• Lateral radius: 4.37 mm

• Dielectric assumed homogeneous and defect-free

• Electrostatic boundary conditions applied

### S3.2 Pt/ZrO₂/BaTiO₃/ZrO₂/Pt Thin-Film Model

• BaTiO₃ thickness: 100 nm

• ZrO₂ barrier layers: 2 nm each

• Electrodes: Pt (high Schottky barrier contact)

• Series dielectric model considered for capacitance calculation

Electric-field-dependent conduction mechanisms were incorporated to evaluate leakage current density.

## S4. Energy Density Calculation

Energy density was calculated using:

W = 1/2 ε₀ εᵣ E²

where ε₀ is vacuum permittivity, εᵣ is relative permittivity, and E is the applied electric field. Breakdown field values obtained from simulation were used to estimate maximum energy density.

## S5. Key Supporting Numerical Values

| Structure | Energy Density (J/cm³) | Leakage Current Density (A/cm²) |
| --- | --- | --- |
| Bulk Ag/BZT/Ag | ≈ 0.84 | 10⁻⁶ – 10⁻⁸ |
| Thickness-Scaled (104 nm) | ≈ 45 | ≈ 10⁻² |
| Pt/ZrO₂/BT/ZrO₂/Pt | ≈ 6 | ≈ 10⁻⁴ |

## S6. Summary

This supplementary information provides additional fabrication details, measurement conditions, and simulation parameters supporting the comparative analysis of bulk, thickness-scaled, and interface-engineered capacitor architectures.